|  | Technical Data Sheet |
| --- | --- |
|  | 027W |

Moisture Curing Silicone

Product Description

FX027W is moisture curing silicone for metals and glass bonding. This product is cured by the moisture in the air. The curing system of this product is alkoxy. It is not stinky and has fast curing properties. This resin is different from the traditional PU which contains isocyanate. This product has good non-yellowing properties. This resin is well suited for electronic devices casting and bonding.

Features

- This product has low viscosity and good leveling properties. It also has surface dryness in 15 minutes.

- This resin has flexible properties and fracture energy.

- This product has stable properties in a wide range of temperature.

- This product is one component adhesive. It is easy to use.

- This resin will fast cure in the air. It can have surface dryness in a short time.

- Stable under -40~230 oC.

- This prodcut complies to the 2011/65/EU RoHS regulations.

Typical Uncured Properties

|  | FX027W |
| --- | --- |
| Composition | Polysiloxane resin |
| Appearance | Liquid |
| Color | White |
| Viscosity*25oC, S14 50rpm, cps | 4,000~6,000 |
| Specific Gravity | 0.98 |
| pH Value | 6~8 |
| Solvent Content, % | 0 |

*This value is for reference. Please refer to COA for the actual value.

Typical Curing Properties

| Surface Dry Time, 25oC, min | 15 |
| --- | --- |
| Curing Depth, 25oC, 50%RH, 15hr, mm | 1.80 |
| Thoroughly Cured Time, 25oC, days | 7 |

Direction of Use

- It should be applied to a clean surface which is free of dirt, grease or mold release. In many cases, a simple solvent wipe is sufficient.

- Pour or brush this product onto the substrates, it does not recommend to stir to avoid interfusing the air. This product will be cured with the air. The curing propeties depend on its thickness, curing temperatrue and relative humidity.

- When casting in thicker components or devices, the resin might not be cured thoroughly at the bottome of the components or devices. This is because the bottom resin is difficult to cure with the moisture. It is recommended to extend the curing time, so that the moisutre can be diffused from the top to the bottom. Another solution is cast the

components or devices twice. Cast the resin to half height of components and devices. When the surface is almost dry and tacky, cast the resin second time.

- Use this product as soon as possible after opening the original packages. When not using, please replace the rid tightly and store in a cool and dry place.

- Cure time on the really part will depend upon fators such as part geometry, materials to be bonded, bondline thickness and humidity. Cure schedule should be confirmed with actual production parts and equipment.

- Cured product will not be harmful to human when it contacts with the skin.

Typical Cured Properties

| Hardness (Durometer) ASTM D2240-03, Shore A | 16 |
| --- | --- |
| Hardness (Durometer) ASTM D2240-03, Shore 00 | 84 |
| Surface Resistivity, Ω | 4.63*1015 |
| Volume Resistivity, Ω‧cm | 4.37*1015 |
| Temperature Range, oC | -40~230 |

Storage and Shelf Life

This product should be kept without any possibility of moisture exposure. Replace the lid immediately after use. Shelf life of this product is six months when stored in dark place below 14~34oC in original, unopened containers.

Caution

Some findings indicate a lack of potential for carcinogenicity with the compositions of this product by long term recurrent application to the skin. However, contact with skin is likely to produce mild transient reddening. It is important to remove adhesive from skin with soap and water thoroughly. DO NOT use solvents for cleaning hands. This product is of moderate acute toxicity by swallowing. If swallowed, call a physician. Avoid contact with eyes. In case of contact, flush with water for at least 15 minutes and get medical attention immediately. For specific information on this product, consult the Material Safety Data Sheet