| Advanced Materials http://www.electrical-insulation-materials.com |  |
| --- | --- |

Aratherm Casting System

| XB 2710 | Resin |  | 100 | pbw |
| --- | --- | --- | --- | --- |
| XB 2711 | Hardener |  | 100 | pbw |

Liquid, prefilled, flame retardant, hot-curing two-component epoxy casting system with excellent thermal conductivity.

| Application | Potting of motors, generators, actuators, modules and sensors |
| --- | --- |

| Processing Methods | Automatic pressure gelation process (APG) Conventional gravity casting process under vacuum. |
| --- | --- |

| Key Properties | High thermal conductivity. Flammability UL 94 V-0 (12 mm). Good thermal resistance. Good resistance to atmospheric and chemical degradation. |
| --- | --- |

| Edition Replaces Edition: - | October 2003 |
| --- | --- |

Product Data (Guideline Values)

XB 2710

High viscosity, highly filled bisphenol A epoxy resin

| Viscosity at 25°C | ISO 12058 | mPa*s | 115000 |
| --- | --- | --- | --- |
| Specific Gravity at 25°C | ISO 1675 | g/cm³ | 2.16 |
| As supplied form | Visual |  | brown paste |
| Flash point | DIN 51758 | °C | 200 |

XB 2711

High viscosity, highly filled pre-accelerated anhydride hardener

| Viscosity at 25°C | ISO 12058 | mPa*s | 45000 |
| --- | --- | --- | --- |
| Specific Gravity at 25°C | ISO 15212 | g/cm³ | 2.14 |
| As supplied form | Visual |  | grey |
| Flash point | DIN 51758 | °C | 145 |

Processing Data (Guideline Values)

Mix Ratio

|  |  |  | Parts by weight |  | Parts by volume |
| --- | --- | --- | --- | --- | --- |
| XB 2710 | Resin |  | 100 |  | 100 |
| XB 2711 | Hardener |  | 100 |  | 100 |

Gel Time, Viscosity and Curing

| Mix Viscosity at 60°C | XB 2710 / XB 2711 | Rheomat MC 20 | mPa*s | 8000 |
| --- | --- | --- | --- | --- |
| Pot life at 60°C (Time to reach 100 Pas) | XB 2710 / XB 2711 | Rheomat MC 20 | min | 400 |
| Gel time at 90°C | XB 2710 / XB 2711 | Gelnorm | min | 35 |
| Gel time at 100°C |  | Gelnorm | min | 20 |
| Gel time at 120°C |  | Gelnorm | min | 7 |
| Minimum Curing Cycle |  | 1hour at 90°C + 1.5 hour at 140°C |

Processing and Storage (Guideline Values)

Remarks

XB 2710 / XB 2711 contain fillers, which tend to settle over time.

It is therefore recommended to carefully homogenize the complete contents of the container before use.

The use of ceramic materials is recommended, due to the abrasiveness of the filler.

Measure (by weight or volume) the Araldite resin and the hardener. Add the hardener to the Aratherm resin, making sure that the required amount of hardener is transferred to the resin. Stir thoroughly until mixing is complete.

Air entrainment during mixing results in pores in the cured resin. Mixing under vacuum or in a metering-mixing machine is the most effective way to prevent air entrainment. Alternatively the static resin – hardener mixture may be deaerated in a vacuum chamber – allowing at least 200 % ullage for the foam to expand.

System Preparation

General instructions for preparing prefilled resin systems

Long pot life is desirable in the processing of any casting resin system. Prefilled components help to shorten the mixing time considerably.

The two components will be mixed in the desired quantity under vacuum and at slightly elevated temperature (50 - 60°C). For the mixing of medium- to high viscous casting resin systems and for mixing at lower temperatures, we recommend special thin film de-gassing mixers that may produce additional self-heating of 10-15 °C as a result of friction. Depending on quantity, mixer device, mixing temperature and application, the mixing time is 0.5 to 1h, under a vacuum of 1 to 8 mbar.

The premixed components packed according to their mixing ratio, could be used per container. In case of filler sedimentation, it is recommended to empty the container completely. Before partial use, the content must be carefully homogenized at elevated temperature. We recommend the same preheating temperature to prevent air enclosures when discharging the components.

In automatic mixing and metering installations, both components will be degassed and homogenized under a vacuum of about 2 mbar in the holding tanks. When degassed, the prefilled products are stirred up from time to time to avoid any sedimentation. After dosing and mixing with a static mixer, the system is fed directly to the vacuum chamber or, in the automatic pressure gelation process, directly into the hot casting mould. By using circular feeding tubes, several casting stations can be served.

Storage Conditions

Store the components in a dry place at RT, in tightly sealed original containers. Under these conditions, the shelf life will correspond to the expiry date stated on the label. After this date, the product may be processed only after reanalysis. Partly emptied containers should be tightly closed immediately after use.

For information on waste disposal and hazardous products of decomposition in the event of a fire, refer to the Material Safety Data Sheets (MSDS) for these particular products.

Mechanical and Physical Properties (Guideline Values)

Determined on standard test specimen at 23°C. Cured for 1h / 90°C and 1.5h / 140°C

| Color of casting |  |  | brown |
| --- | --- | --- | --- |
| Glass transition temperature | ISO 11359-2 | °C | 120 |
| Density | ISO 1183 | g/cm3 | 2.1 |
| Flexural strength | ISO 178 | MPa | 78 |
| Elongation at break | ISO 178 | % | 0.6 |
| Flexural modulus | ISO 178 | MPa | 3000 |
| Hardness | ISO 868 | Shore D | 92 |
| Critical stress intensity factor | PM 216-0’/89 | MPa*m1/2 | 2.2 |
| Specific energy at break | PM 216-0’/89 | J/m2 | 300 |
| Coefficient of thermal expansion Alpha 1 < Tg Alpha 2 > Tg | ISO 11359-2 | ppm/K | 24 67 |
| Thermal conductivity | ISO 8894 | W/m*K | 1.5 |
| Flammability | UL 94 |  | V-0 (12mm) |

Electrical Properties (Guideline Values)

Determined on standard test specimen at 23°C. Cured for 1h / 90°C and 1.5h / 140°C

| Dielectric loss factor (tan  50Hz, 25°C) | IEC 60250 | % | 1.2 |
| --- | --- | --- | --- |
| Dielectric constant (r 50Hz, 25°C) | IEC 60250 |  | 4.7 |
| Specific volume resistivity ( 25°C) | IEC 60093 |  cm | 6.1 x 1014 |

Industrial hygiene

Mandatory and recommended industrial hygiene procedures should be followed whenever our products are being handled and processed. For additional information please consult the corresponding Safety Data Sheets and the brochure "Hygienic precautions for handling plastics products of Huntsman” (Publ. No. 24264/e).

Handling Precautions

| Safety precautions at workplace: Protective clothing Gloves Arm protectors Goggles/safety glasses Respirator/dust mask Skin protection: Before starting work After washing Cleaning of contaminated skin Clean shop requirements Disposal of spillage Ventilation: Of workshop Of workplace | Yes. Essential. Recommended when skin contact likely. Yes. Recommended. Apply barrier cream to exposed skin. Apply barrier or nourishing cream. Dab off with absorbent paper, wash with warm water and alkali-free soap, then dry with disposable towels. Do not use solvents. Cover workbenches, etc. with light coloured paper. Use disposable beakers, etc. Soak up with sawdust or cotton waste and deposit in plastic-lined bin. Renew air 3 to 5 times an hour. Exhaust fans. Operatives should avoid inhaling vapors. |
| --- | --- |

First Aid

Contamination of the eyes by resin, hardener or casting mix should be treated immediately by flushing with clean, running water for 10 to 15 minutes. A doctor should then be consulted.

Material smeared or splashed on the skin should be dabbed off, and the contaminated area then washed and treated with a cleansing cream (see above). A doctor should be consulted in the event of severe irritation or burns. Contaminated clothing should be changed immediately.

Anyone taken ill after inhaling vapours should be moved out of doors immediately. In all cases of doubt call for medical assistance.

| Vantico Ltd Advanced Materials ®Registered trademark | All recommendations for use of our products, whether given by us in writing, verbally, or to be implied from results of tests carried out by us are based on the current state of our knowledge. Notwithstanding any such recommendations the Buyer shall remain responsible for satisfying himself that the products as supplied by us are suitable for his intended process or purpose. Since we cannot control the application, use or processing of the products, we cannot accept responsibility therefore. The Buyer shall ensure that the intended use of the products will not infringe any third party's intellectual property rights. We warrant that our products are free from defects in accordance with and subject to our general conditions of supply. |
| --- | --- |