|  | Technical Data Sheet |
| --- | --- |
|  | PT934-2 |

Removable Photo-curing Adhesive

Product Description

PT934-2 is removable photo-curing adhesive. It is used for protecting some materials temporarily. When removing this product, pull up one side of the cured resin, it is easy to remove all the cured resin from the materials.

Typical Uncured Properties

|  | PT934-2 |
| --- | --- |
| Composition | Acrylic resin |
| Appearance | Liquid |
| Color | Blue |
| Viscosity* 25oC, S14 100rpm, cps | 7,000~11,000 |
| Thixotropic Index | >4 |
| Certificate | RoHS |
| Application | Dispensing |

*This value is for reference. Please refer to COA for the actual value.

Typical Curing Properties*

| Curing Equipment: Mercury Lamp / Halogen Lamp |
| --- |
| Recommended Wavelength, nm | 310~420 |
| Main Wavelength, nm | 365 |
| Minimum Light Intensity, mW/cm2 | > 50 |
| Minimum Light Energy, mJ/cm2 | 1,500~2,000 |

| Curing Equipment: LED Light |  |
| --- | --- |
| Recommended Wavelength, nm | 365~420 |
| Wavelength, nm | 365 |
| Minimum Light Intensity, mW/cm2 | > 50 |
| Minimum Light Energy, mJ/cm2 | 2,000~3,000 |

*The minimum light energy is for reference.

Direction of Use

- The surface of the resin contact should be clean.

- Apply adhesive to one or both substrates to be bonded. The contact surface should be completely flattened until the resin cured.

- Cure time on the really part will depend upon fators such as part geometry, materials to be bonded, bondline thickness and efficiency of the UV light. Cure schedule should be confirmed with actual production parts and equipment.

- Please standardize the UV lamp intensity and illumination. Over exposure will not affect the resin properties, but the resin properties will be changed if there is not enough exposure. The resin may have lower reaction rate and may not pass the envrionmental test experiments.

- This product may cause skin irritation to sensitive personnel.

Typical Cured Properties

| Durometer Hardness ASTM D2240-03, Shore A | 69 |
| --- | --- |
| Elongation, % | 265 |

Storage and Shelf Life

The product should be stored in cool and dark place. Avoid to contacting with sunlight or ultraviolet. Replace the lid immediately to keep away from any possibility of light exposure after using. Shelf life of this product is six months when stored in room temperature from 14oC ~34oC in original, unopened containers.

Caution

Some findings indicate a lack of potential for carcinogenicity with the compositions of this product by long term recurrent application to the skin. However, contact with skin is likely to produce mild transient reddening. It is important to remove adhesive from skin with soap and water thoroughly. DO NOT use solvents for cleaning hands. This product is of moderate acute toxicity by swallowing. If swallowed, call a physician. Avoid contact with eyes. In case of contact, flush with water for at least 15 minutes and get medical attention immediately. For specific information on this product, consult the Material Safety Data Sheet.